## Slide 1
Synthesis of Activated Carbon/Sodium Alginate Composites for Wastewater Treatment
SMACUMED International Conference on Water-Energy-Food-Ecosystem Nexus in the Mediterranean Region
(WEFE 2023)
By Yaacoubi Fatima Ezzahra
PhD candidate
Laboratory of applied chemistry and biomass
Department of chemistry,
Faculty of sciences Semlalia-Marrakesh (FSSM)

## Slide 2
INTRODUCTION
Valorization of biomass derived from local lignocellulosic agricultural waste
Chemical analysis (%) | 
Lignin | 37.8
Hemicellulose | 19.7
Cellulose | 17.8
Volatile | 70.5
Ash | 2.25
Fixed Carbon | 20.2
WEFE2023

## Slide 3
Materials & methods
Preparation of activated carbon by chemical activation
1. Impregnation of biomass using KOH
2. One-step activation
Washing and Drying
WEFE2023

## Slide 4
Materials & methods
Preparation of activated carbon/sodium alginate (AC/Alg) composites
WEFE2023

## Slide 5
Materials & methods
Surface area (m2/g) | Average pore size (nm) | Pore volume (cm3/g)
374.82 | 1.40 | 0,131
characterization
SEM analysis
FTIR spectra
BET analysis
pH at the zero point of charge
Conducted on beads before and after MB adsorption
WEFE2023

## Slide 6
Results & discussion
Infrared spectroscopy analysis is performed on AC/Alg composites before and after MB adsorption
All adsorption tests were performed at a pH of 6, higher than the , using 10mg of the adsorbent material per 100 ml of methylene blue solution.
WEFE2023

## Slide 7
Results & discussion
Modelization
Adsorption kinetics
Adsorption isotherms
The adsorption kinetics of MB follows the pseudo-1st order model, with a Qmax of 586 mg/g according to the Langmuir model
WEFE2023

## Slide 8
Results & discussion
Reusability tests
The beads were carefully washed with 0.1 M of hydrochloric acid to remove the adsorbed dye molecules;
This adsorption and washing cycle was repeated for a total of 5 cycles.
WEFE2023

## Slide 9
Conclusion
this study contributes to the understanding of the adsorption behavior of methylene blue and the potential application of AC/Alg-Na composites as effective and reusable adsorbents.
Approximately 60% of methylene blue was removed while reaching a maximum adsorption capacity of 586 mg/g according to the Langmuir model
WEFE2023